# PAINTING

## Material

### All paints shall be approved by the Consultant for colour, quality and type. All painting work shall be carried out in accordance with the paint manufacturer’s specifications unless otherwise directed by the Consultant.

### All paints and finishes used for the project shall be manufactured by or under license from one of the following manufacturers;

### (a)	Nippon Paint

### (b)	Sigma Paint

### Paint shall be ready mixed and all paints, varnishes, enamels, lacquer stains, paste fillers and similar materials shall be delivered to the site in the original containers with the seals unbroken and labels intact. Each container shall give the manufacturer’s name, type of paint, colour of paint and instructions for reducing. Thinning shall be done only in accordance with the manufacturer’s directions.

### Use of product by the same manufacturer shall be a general rule in each stage of work in this Specification.

### Colour, lustre, colour scheme, finish shall be decided by the Consultant after checking sample paint test.

### The painting shall be performed by experienced and competent painter.

### Where the walls are specified to be painted, all columns arises, groove, rough surfaces, reveals, soffits and returns, etc. shall be included. No extra shall be payable.

## Definition of Terminology

Surface Sealing

Surface to be painted shall be sealed to have uniform suction and prevent lye from oozing out.

Spot Puttying

All cracks and depressions shall be filled flush with putty.

Puttying

All surfaces to be painted shall be puttied uniformly flat surface.

Spot painting

Spot puttied area shall be touched up by paint

Touch-up

Any damaged area after the prime coat has been applied shall be touched up

Drying hour

The drying time of double-coated paint shall be measured at the temperature of 20°C and humidity of 70%.

Amount of paint

The amount shall be standard amount of paint itself not including thinner. It shall increase or decrease depending on shape and surface condition in the process of painting.

## Paint Finish Symbols

OP			Synthetic resin mix paint finish

VP			Solvent-polyvinyl chloride resin paint finish

EP			Polyvinyl acetate resin emulsion paint finish

AEP			Synthetic resin emulsion paint finish

CL			Clear lacquer finish

EXP			Epoxy resin paint finish

Stipple (OP)		Stippled finish (oil mix paint finish)

Stipple (EP)		Stippled finish (polyvinyl acetate resin emulsion paint finish)

## Painting in General

### Preparation of Paint

#### Mixing: Paint content with pigment shall be thoroughly stirred to make a uniform consistency.

#### Thinning: Portable water shall be used for thinning of emulsion paint and water-soluble paint. Proper thinner, product of the same manufacturer as paint, as a rule, shall be used for other types of painting. Percentage of thinning and viscosity shall be conducted with direction of manufacturer or catalogue as they vary with the method of paint, temperature, type of material to be painted.

#### Allowable period of Use: Paint mixed with more than 2 types shall be used with direction of a manufacturer or catalogue as allowable period of use, mixing ratio and mixing method vary. The paint which has passed allowable period of use shall not be used.

### Conditions of Painting

#### Work shall not be executed in the following situations

#### When humidity is above 85%

#### When raining or it is forecast

#### When dusts are present

#### When temperature of surface is high under hot weather and bubbles     are likely to develop on the painted surface.

#### Conditions of Surface to be painted: Work shall not be executed or proper means shall be taken in the following situations.

#### When surface is damp and wet

#### When condensation (is likely to) develop on the surface.

#### All nail holes on veneer, board. etc., shall be covered with proper rust-proof paint before the subsequent painting is applied in accordance with this specification.

### Performance

#### Paint shall be evenly and uniformed applied on the surface. Areas of difficult application such as pointed part, internal angle, welded part, etc. shall be thoroughly painted and double coated as necessary to deep uniform coating thickness.

#### Painting shall be properly done by carefully selecting the painting method by the shape of surface and types of paint.

### Protection

#### Dangerous material such as paint, thinner, etc., excluding emulsion paint and water-soluble paint shall be kept in accordance with regulations concerned.

## Procedure of Painting

### Exterior - Surface of Mortar, Plaster and Concrete

AEP- Synthetic resin emulsion paint.

| Coating Process | No. of Coats | Type of Paint | Drying hour | Amount (kg/m²) |
| --- | --- | --- | --- | --- |
| 1. Surface preparation |  | Dry, clean and free from impurities |  |  |
| 2. Surface sealing | 1 | Sealer for emulsion paint | longer than 4 hours |  |
| 3. Puttying |  | Putty for emulsion paint |  |  |
| 4. Grinding |  | Grind with proper grinding tool |  |  |
| 5. Spot painting |  | Synthetic resin emulsion paint |  |  |
| 6. Second coating | 1 | Synthetic resin emulsion paint | longer than 4 hours | 0.10-0.13 |
| 7. Finish coating | 2 | Synthetic resin emulsion paint | longer than 4 hours | 0.10-0.13 |

Notes:

Degree of dryness on the surface to be painted shall be kept under 6% in water content and below pH 9.5

Puttying and sanding process shall allow omitting depending on the conditions of the surface.

Drying time of putty shall be long enough for sanding to proceed.

Amount of sealer for surface sealing shall be adjusted with direction of the Consultant as it varies with the surface conditions.

### Exterior - Iron Products in General

OP - Synthetic resin mix paint

| Coating Process | No. of Coats | Type of Paint | Drying hour | Amount (kg/m²) |
| --- | --- | --- | --- | --- |
| 1. Surface preparation |  | Completely remove rust, moisture, oil and other impurities by sander, cleaner and surface. |  |  |
| 2. First Coating 24 hours | 1 | Rust proof oil paint | longer than 24 hours | 0.13-0.15 |
| 3. Touch-up |  | Touch-up rustproof oil paint |  |  |
| 4. First Coating | 1 | Rustproof oil paint | longer than 24 hrs | 0.13-0.15 |
| 5. Second coating | 1 | Synthetic resin mix paint | longer than 15 hrs | 0.11-0.15 |
| 6. Finish coating | 1 | Synthetic resin mix paint | longer than 15 hrs | 0.11-0.15 |

Note:

Paint for touch-up painting shall be the same as used for first coat in process No. 2

### Exterior - Wood

OP - Synthetic resin mix paint finish

| Coating Process | No. of Coats | Type of Paint | Drying hour | Amount (kg/m²) |
| --- | --- | --- | --- | --- |
| 1. Surface preparation |  | Clean and sand to plane surface |  |  |
| 2. Knot treatment | 1-2 | Lacquer varnish | longer than 24 hours |  |
| 3. First coating | 1 | First coat paint of oil mix paint | longer than 24 hrs | 0.13-0.15 |
| 4. Second Coating | 1 | Oil mix paint | 24 hrs | 0.11-0.13 |
| 5. Finish coating | 1 | Oil mix paint | longer than 24 hrs | 0.11-0.13 |

Note:

  - Puttying and sanding shall be done after process No.2 when there are cracks, etc. on the surface putty shall be oil-putty, but drying time shall vary depending on conditions.

### Interior - Mortar, board, etc.

Stipple (EP) - Polyvinyl acetate resin emulsion paint finish

| Coating Process | No. of Coats | Type of Paint | Drying hour | Amount (kg/m²) |
| --- | --- | --- | --- | --- |
| 1. Surface preparation |  | Dry, clean and free from impurities |  |  |
| 2. Surface sealing | 1 | Sealer for emulsion paint | longer than 4 hours |  |
| 3. Puttying |  | Putty for emulsion paint |  |  |
| 4. Grinding |  | Grind with proper grinding tool |  |  |
| 5. Spot painting |  | Second coating paint of polyvinyl acetate resin emulsion paint |  |  |
| 6. Second Coating | 2 | Polyvinyl acetate resin emulsion paint | longer than 4 hrs | 1.11-0.13 |
| 7. Finish Coating | 1 | Polyvinyl acetate resin emulsion paint for stipple-finish | longer than 4 hrs | 0.25-0.35 |

Notes:

Degree of dryness on the surface to be painted shall be kept under 6% in water content and below PH 9.5

Puttying and sanding process shall allow omitting depending on the conditions of the surface.

Drying time of putty shall be long enough for sanding to proceed.

Amount of sealer for surface sealing shall be adjusted with direction of the Consultant as it varies with the surface conditions.

### Interior - Mortar, plaster, concrete, etc.

VP Solvent - Polyvinyl chloride resin paint finish

| Coating Process | No. of Coats | Type of Paint | Drying hour | Amount (kg/m²) |
| --- | --- | --- | --- | --- |
| 1. Surface preparation |  | Dry, clean and free from impurities |  |  |
| 2. Surface sealing | 1 | Sealer for emulsion paint | longer than 2 hours |  |
| 3. Puttying |  | Putty for polyvinyl chloride resin paint |  |  |
| 4. Grinding |  | Grind with proper grinding tool |  |  |
| 5. Spot painting |  | Solvent-polyvinyl chloride resin enamel emulsion paint |  |  |
| 6. Second Coating | 1 | Solvent-polyvinyl chloride resin enamel emulsion paint | longer than 4 hrs | 0.11-0.14 |
| 7. Finish Coating | 2 | Solvent-polyvinyl chloride resin enamel emulsion paint | longer than 4 hrs | 0.11-0.14 |

Notes:

Degree of dryness on the surface to be painted shall be kept under 6% in water content and below PH 9.5

Puttying and sanding process shall allowed to omit depending on the conditions of the surface.

Drying time of putty shall be long enough for sanding to proceed.

Amount of sealer for surface sealing shall be adjusted with direction of the Consultant as it varies with the surface conditions.

### Interior - Mortar, plaster, concrete, etc.

EP Polyvinyl acetate resin emulsion paint finish

| Coating Process | No. of Coats | Type of Paint | Drying hour | Amount (kg/m²) |
| --- | --- | --- | --- | --- |
| 1. Surface preparation |  | Completely remove rust, moisture, oil and other impurities by sander, cleaner and surface |  |  |
| 2. First Coating | 1 | Synthetic resin rust-proof. Red lead-type, lead compound-type | longer than 24 hrs | 0.18-0.22 0.13-0.15 |
| 3. Touch-up |  | Touch-up rust proof paint |  |  |
| 4. First Coating | 1 | Synthetic resin rust-proof paint. Red lead-type, Lead compound-type | Longer than 24 hrs | 0.18-0.22 0.13-0.15 |
| 5. Second Coating | 1 | Synthetic resin mix paint | longer than 15 hrs | 0.11-0.13 |
| 6. Finish Coating | 1 | Synthetic resin mix paint | longer than 15 hrs | 0.11-0.13 |

| Coating Process | No. of Coats | Type of Paint | Drying hour | Amount (kg/m²) |
| --- | --- | --- | --- | --- |
| 1. Surface preparation |  | Dry, clean and free from impurities |  |  |
| 2. Surface sealing | 1 | Sealer for emulsion paint | longer than 4 hrs |  |
| 3. Puttying |  | Putty for emulsion paint |  |  |
| 4. Grinding |  | Grind with proper grinding tool |  |  |
| 5. Spot painting |  | Polyvinyl acetate resin emulsion paint |  |  |
| 6. Second Coating | 1 | Polyvinyl acetate resin emulsion paint | longer than 4 hrs | 0.11-0.13 |
| 7. Finish Coating | 1 | Polyvinyl acetate resin emulsion paint | longer than 4 hrs | 0.11-0.13 |

Notes:

Degree of dryness on the surface to be painted shall be kept under 6% in water content and below PH 9.5

Puttying and sanding process shall allow omitting depending on the conditions of the surface.

Drying time of putty shall be long enough for sanding to proceed.

Amount of sealer for surface sealing shall be adjusted with direction of the Consultant as it varies with the surface conditions.

### Interior - Iron products, steel.

OP - Synthetic resin mix paint

Notes:

Paint for touch-up painting shall be the same as used for first coat in process No.2

When oil rust-proof paint is used instead of synthetic resin rust proof, its specification shall conform to No. 5 and No.6.

### Floor - Concrete and Mortar

EXP - Epoxy resin paint finish

| Coating Process | No. of Coats | Type of Paint | Drying hour | Amount (kg/m²) |
| --- | --- | --- | --- | --- |
| 1. Surface treatment |  | Dry, clean and free from impurities |  |  |
| 2. First coating | 1 | First coating paint for epoxy | Longer than 24 hrs |  |
| 3. Finish Coating | 2 | Epoxy resin paint | Longer than 24 hrs |  |

Notes:

Degree of dryness on the surface to be painted shall be kept under 6% in water content and below PH 9.5.

Amount of paint and number of paint shall be as directed by the Consultant as they vary with the conditions of surface and required thickness of coating.

Painted surface shall be kept out of use for more than 7 days after application of final coat.